Product code: 	P85

Description:		P85 round paper board container 85cc

Dimensions:		Capacity 		85cc

Carton grammage	241g/m² +/- 5%

Rim diameter		73.5mm +/- 5%

Bottom diameter	60mm +/- 5%

Height			45mm +/- 5%

Weight			4.1g +/-5%

Material:		PE coated board suitable for direct food contact.

Recyclable where facilities exist, check with local council.

Intended use for packaging dry, aqueous, acidic, low alcoholic and fatty foodstuffs.

Decoration:		Plain, or bespoke print to customers’ requirements

Packing:		1740 units per box	58 units per row	30 rows per box

22 boxes per pallet

Box dimensions:	450 x 375 x 515mm

Pallet Dimensions:	Length 1200mm

Width 800mm

Height 144mm

Weight 12-21kgs

Stacking:	Maximum 1 pallet high. Customers should make internal trials to determine the viability of stacking and transportation once filled.

Quality:	Deviations in the product specifications of 0.025% (i.e. 25 items per 100,000) are considered acceptable in the industry and therefore cannot be construed as defect.

Works orders including full traceability information will be held for a minimum period of twelve months from the date of manufacture.

The material complies with the material and articles in contact with food regulation (EC)1935/2004. The extrusion coated paperboard is produced in accordance with Commission Regulation (EC) 2023/2006 on good manufacturing practices for materials and articles intended to come into contact with food. All the materials used in the extrusion coating comply with the relevant requirements of Commission Regulation (EU) 10/2011 on plastic materials and articles intended to come into contact with food.

The user of the product is responsible for ensuring that the finished food packaging complies with the applicable migration limits in the food itself under actual conditions of use.

Issue 1       25/02/2026

Technical Data Sheet

P85 Round paper board container 85cc